LAUDESCHER LINEA SLATTED ACOUSTIC WALL CLADDING

K13/170 NBS TECHNICAL SPECIFICATION

ACOUSTIC PANELS TO: 	……………………………………………………….

Refer to drawings: 	……………………………………………………....

Manufacturer and reference: 	LAUDESCHER LINEA timber slatted acoustic wall cladding

Design reference:		LAUDESCHER LINEA 2.6.5

Acoustic Products Ltd

70c High Street

Whitstable

Kent

CT5 1BB

Tel	01227 281140

Fax	01227 281141

Email	enquiries@acoustic-products.co.uk

Total thickness: 			95 mm

Slat section: 				20 x 68 mm

Facing side: 				20 mm

Slat thickness: 				68 mm

Rear black wooden counter-slats: 	34 x 45 mm

Spacing between slats: 			54 mm

Average void area: 			73%

Reaction to fire: 			B-s1,d0 / B-s2,d0 as defined in standard EN 13501-1

D-s1,d0 untreated wood  as defined in standard EN 13501-1

Solid wood:				Pine / Douglas Fir / Oak

Finishing:				Clear varnish / Wax Colour / Wax Colour MC

Panel sizes & quantities:		Pre fabricated units in standard sizes of 1880mm x 600mm

and/or 1265mm x 600mm or to order.

Installation:              		In accordance with the manufacturer’s recommendations all as

detailed in the LAUDESCHER LINEA Installation Manual available to download at: https://www.acoustic-products.co.uk/movable-wall-technical-downloads